Abstract-- This paper describes a decade of work on digital imaging for museums. In 1989-92, the EU-funded VASARI project produced a digital imaging system that made colour-calibrated images of up to 20k x 20k pixels directly from paintings. It used seven colour-separation bands in the visible region, resulting in an average colour error of around 1 Eab unit. These images have since been used to monitor the condition of paintings, to document paintings during conservation treatment, including predicting appearance after cleaning, to reconstruct the original appearance of paintings in which pigments have faded, to assess whether paintings have been damaged during transportation, in estimations of the surface reflectance spectra, and in the printing of high-quality reproductions. We have applied similar techniques to museum infrared and X-ray imaging. To manage the images produced by the VASARI system, an image-processing package has been developed that is tailored for very large colorimetric images. This package has since been used in several other projects, including a remote image viewer designed to provide internet access to high-resolution images. The paper explores these developments, and gives details of the current generation of VASARI-derived systems, set in the context of the state-of-the-art for museum imaging.

10 years of Art imaging research

Kirk Martinez, John Cupitt, David Saunders, Ruven Pillay

Index Terms-- imaging, image processing, museum, painting, colorimetry

# Introduction

This paper summarises roughly a decade of work developing imaging systems for digitising works of art, particularly paintings. Although these systems were built specifically to image paintings in museums and galleries, the techniques used are more widely applicable. The expertise needed for their realisation was drawn from a number of fields, including optics, mechanical engineering, image processing, colour science, computer science and painting conservation.

At the end of the 1980s, digital imaging was developing at a rapid pace. New devices such as CCDs made it possible to consider replacing film photography and spectrophotometry [1] with direct digital imaging [2]. Digital imaging has compelling conservation advantages over film: its permanence means that damage to the object caused by rephotography is reduced, its accuracy ensures that images taken many years apart may be compared, and its transmissibility makes sharing information with conservators in partner institutions far easier.

We expected the colour accuracy to be lower than spectrophotometry, but we felt that the ability to detect colour change anywhere on the surface was more important. With spot techniques, such as spectrophotometry, you have to decide now which areas of the painting you expect to change in colour in the next 20 years: not an easy problem. Imaging techniques avoid this difficulty by simply measuring the entire surface.

At the time it seemed that the major question mark over digital imaging was whether its spatial resolution would be sufficient. From the point of view of a photographer, to replace a standard 10" x 8" transparency film resolving 40 lines pairs per millimetre would require an image of around 16k x 20k pels. From the point of view of a conservator, the smallest feature of a painting that you might reasonably want to record is the pattern of cracks (cracquelure) in the surface layers of paint. Examinations of X-radiographs showed that cracks measuring around 0.1 mm are typical, therefore a resolution of 20 pels per millimetre on the surface of the painting is required. There are microscopic features which are of interest but that ould mean scanning the whole painting to an extremely high resolution. For a 1m by 1m painting, 20 pels/mm corresponds to 20k x 20k pels. This was far higher than any imaging device available in 1989.

Another difficult question was the format to be used for storing colour information. We needed to be certain that our measurements would be useful in 5 or even 20 years time, when our successors would need to compare our readings against their own, almost certainly made with very different equipment. The ideal goal was to store reflectance spectra but until recently CIE Lab [3] values were stored.

2. The VASARI Project

In 1989 we were part of a group that was interested in exploring the limits of digital imaging. With colleagues from other European museums and universities we started a European Community-supported project called VASARI (Visual Arts System for Archiving and Retrieval of Images) [4,5,6]. The project aims were to produce an imaging system good enough to replace technical photography of paintings, and to use this system to look for changes in paintings on display, or changes occurring during transportation between museums [7].

The project resulted in the production of two imaging systems: one installed in the National Gallery in London optimised for colour measurement, and the second in the Doerner Institute in Munich optimised for monochrome transportation damage assessment. As a result of a further European initiative, a third scanner, similar to that in London, was installed at the Galleria degli Uffizi in Florence.

## Hardware design

At an early stage of the design we decided that the painting should be scanned while vertical, since the shape of a canvas painting changes when it is laid flat. This was in contrast to comparable systems, such as the innovative scanner that had already been developed to digitise the US Constitution in Washington [8]. As well as maintaining the paintings in their normal position, this would also help to prevent accidental damage if sections of the prototype scanner were to drop off.

Partners at ENST (Ecole Nationale Supérieure des Télécommunications, Paris) carried out simulations using the spectra of known pigments to define an ideal set of 7 filters for imaging paintings. Unfortunately these ideal theoretical filters were not practical or affordable, so as a second choice we selected seven broad-band Gaussian filters with peak transmittances at 400 to 700nm in 50nm intervals and a band width at half maximum transmittance of 70nm. Simulations showed that this Gaussian filter set was only slightly worse than the ideal set.

Interference filters are sensitive to heat, making it impossible to get enough light through a single filter to illuminate an entire painting. The filters we chose were also rather thick, and varied greatly in thickness, making them very hard to use inside the optical path of a camera. Our solution was to use fibre-optic guides to pass light through a single filter, and then illuminate a small patch of the painting. This had the additional important advantage of exposing the painting to far less light during scanning. Figure 1 shows a schematic of the lighting system.

Since we only had enough light to illuminate a small part of the painting at any time, we were forced to image the painting in many small pieces. One obvious design idea is to use a stationary camera and lighting system, and to move the painting in front of the camera on a computer-controlled easel. Again, for safety reasons, we felt that we had to keep the painting stationary. This meant that we had to transport the entire camera and lighting system (about 15kg) across the surface of the painting. We were unsure what accuracy we would require for this motion, so when we commissioned the positioning system, we asked for 50 microns.

We selected the highest resolution camera we could afford, the Kontron ProgRes 3000 [9]. This camera could take a 3k x 2k pel colour image in about 30 seconds, fast for the time. We bought a monochrome version and selected a lens with almost no geometric distortion, and low chromatic aberration. Stitching software would be written to join the image tiles and we wanted to avoid complex geometric corrections.

## Software design

We implemented an automatic acquisition and calibration package for the VASARI scanner. The painting to be scanned was placed on the easel, its dimensions were entered, any adjustments to the acquisition parameters were made, and scanning started. The system was written in C under Unix with later additions of an X-Windows interface an C++ for the calibrator.

### Calibration targets

A number of calibration targets were scanned before acquisition proper started. First, the system prompted the user to cover the camera lens before taking a dark current image. This was subtracted (with an offset to prevent clipping of negative noise) from all subsequent images.

The resolution of the image depended on the camera-to-object distance, which varied slightly between acquisitions. The first target was a vertical white line on a black background. The camera moved left and right a small amount, and measured the movement of the image of the line on its sensor. Scanning resolution was calculated from this. This resolution figure was used to guide the movement of the camera over the painting, to ensure that there was a small overlap between neighbouring images.

The fibre-optic lighting system did not produce perfectly uniform illumination. The next calibration target was a polished sheet of PTFE. An image of the PTFE sheet was used to correct for variations in pixel sensitivity, illumination homogeneity, and lens shading in all subsequent images.

A Macbeth ColorChecker Chart (see figure 2) was used for colour correction. Although this chart has only 24 patches, the patches are made from complex dye mixtures rather than being produced photographically or printed. This gives them spectral curves similar to the pigments found in paintings. We cut the chart tiles into quarters to fit within the field of view of the camera (a small version is now available).

### Painting acquisition

The camera was then moved over the surface of the painting, capturing seven monochrome images of 3k by 2k pels at each position. The camera's field of view covered an area on the painting of about 17cm x 13cm, giving a resolution of approximately 18 pels per millimetre. Scanning took around three hours for a 1m x 1m object. Figure 3 shows the scanner shortly after construction.

## Processing and storage

After the painting had been captured, a second processing stage was run. This used the images captured during acquisition to automatically calculate a single very large output image. This is stored uncompressed as CIELab in our own simple VIPS file format.

First, the images of the Macbeth chart [10], combined with spectrophotometric measurements of the chart patches, were used to determine a transformation, which mapped the seven bands of the scan to D65 CIE XYZ colourspace. The camera outputs are initially linearised with respect to Y.

It is assumed that the standard observer curves used to generate CIEXYZ can be constructed with a linear combination of the gaussian filters we used. Then a simple linear model is used where the camera values F are related to the CIEXYZ colour values of the test chart V in a simple linear system where K is an unknown set of coefficients.

or in full form:

XY

The colour calibration calculates the values of kX1 to kZ7 in the conversion matrix (K) above. This is achieved by imaging n (where n7) colour standards (with known XYZ values) through each of the filters. The matrix (Φ) representing the camera response to each colour in the chart, through each filter (f11,f21, ... f7n) is combined with the known XYZ values for the n colours (X1,Y1,Z1, ... Xn,Yn,Zn), matrix (V), to generate the least mean square solution for the conversion matrix K:

K  =  (ΦTΦ)−1ΦTVT

Where:

Φ  =  f11f21..f71f12f22..f72......f1nf2n..f7n   V  =  X1Y1Z1X2Y2Z2......XnYnZn

K is then used to convert images of paintings into calibrated XYZ values. The equation for K above gives a least-mean-squares solution which usually gives an average colour error on the Macbeth chart of 1 ab units. Most colours from the chart are calibrated very well but others may be as far as 5 ab units in error.

Next, each of the image tiles making up the painting were transformed to CIE Lab, and saved back to disc. Finally, the overlapping areas between tiles were analysed, and the correlation surfaces used to find a set of joins that minimised errors between neighbouring subimages [11]. The image patches are mosaiced together using normalised correlation of the overlapping areas. In order to ensure that the correlation uses image areas which are not smooth, a laplacian high-pass filter is applied to the overlaps and around 20 areas of high detail found. These smaller areas then correlated with slightly larger (by 20 pels typically) corresponding areas on the other image. These search-area limiting techniques, together with knowledge of the overlap size (typically 100 20 pels) increases the success rate. By using three main regions for correlation: top, centre and bottom, correlated features provide points which are fitted to a line, giving the relative position and rotation of the two images. The patches are then joined by using a raised cosine blender. This technique is very successful and has also been applied to infra-red and X-ray images.

## Enhancements to VASARI since 1993

We have continued to improve the VASARI scanner since its original completion. We have upgraded the camera A/D to 12 bits/pel in order to reduce quantisation effects and made significant improvements to the colour calibration software.

The original VASARI software did a simple least mean square (LMS) fit from the Macbeth chart measurements to find a 7 x 3 matrix which mapped the seven scanner bands to CIE XYZ. Unfortunately, a solution which is minimal with respect to errors in XYZ colour space, is not minimal visually. We have replaced this with a singular value decomposition to get an initial solution, followed by an iterative scheme using Powell’s multidimensional minimisation method [12]. This minimises a function which is a combination of ab and the standard deviation of errors. We have also added a preprocessing stage which examines the Macbeth greyscale and adjusts the scale and offset for each band to try to get the black and white points in exactly the right place. This does not use the black or white chart patches as they are the most prone to errors.

Another factor which we did not consider carefully enough in the original design is the issue of gloss versus matt finish. The paintings in the National Gallery are almost all finished with a modern synthetic medium gloss varnish. Although the Macbeth chart is a good spectral match for paintings, it has a very flat matt surface finish. This difference leads to errors in the black point determination, resulting in images of paintings with the black point too low. We have coated our Macbeth charts with a painting varnish to remove this problem.

A significant problem we did not anticipate is that of optical scatter. Imperfections in the camera optics will scatter some of the light from bright areas of the field to dark areas. Since the camera and lights move over the painting, a dark area of the surface might be next to a white patch in one frame, and not in an adjacent frame. This can lead to an obvious join line. Scatter is an important factor limiting the accuracy of imaging techniques for colour measurement.

We have been able to reduce this problem by observing that the amount of light added to dark areas of the field of view is approximately proportional to the average of the field of view. In other words:

camera_response(x,y)  light_from_object(x,y) + mean(field) * scatter_coeff

We can calculate scatter_coeff by imaging patches of the same reflectivity against backgrounds of different reflectivity. Applying this correction to all the fields in a scan removes visible join lines.

The scanner was refurbished after a laboratory move. A new easel was constructed, which can hold paintings up to 2m x 2m, sliding a 1m x 1m section in front of the scanner. The number of filters was increased to 12, covering 450nm to 1000nm in 50nm steps in order to add near-infra-red capability. The lighting system was redesigned for the third time, which will double the flux. Figure 4 shows the VASARI scanner as it appeared in 2000.

# The MARC Project

In 1993-6, the European Community-supported MARC [14] project (Methodology for Art Reproduction in Colour) applied VASARI results to the printing of high-quality art books. Within the project, a new scan-back camera was designed and built by Drs Udo and Reimar Lenz at the Technical University in Munich [13], while the higher-level camera software was developed in London by the authors. The MARC camera used a similar, masked CCD to that in the ProgRes camera, but with a combination of macro and micro positioning to cover the image plane of a 6 x 6cm camera at resolutions of up to 20k x 20k pels.

The MARC camera used a RGB colour sensor and 12 bit A/D converter, making it less accurate than the VASARI scanner because of the reduction in the number filters. Offsetting this disadvantage was its portability, ability to image objects of any size, ability to image 3D objects, and its similarity to a conventional film camera, making the device familiar to photographers. It was also much faster than VASARI, taking around 40 minutes for a 10k by 10k scan.

The MARC camera software used colour calibration techniques similar to the VASARI scanner. A Macbeth chart was placed in front of the object prior to each session, and readings from the chart used to calibrate the images to CIE Lab colour space. With HMI lamps, the average colour error on the Macbeth chart was around 2 ab units. Figure 5 shows the MARC camera.

Crosfield Electronics, one of the MARC partners, developed a package for calibrating and printing to a conventional 4-colour offset press. To demonstrate the technology, the MARC project produced a colorimetric catalogue of Flemish Baroque Painting [15].

# The VIPS image processing library

We designed and implemented our own image processing system in the course of the VASARI and MARC projects. We needed an image processing package capable of processing very large (around 1Gbyte) colorimetric images on rather modest hardware. The first SUN workstation we used for development only had a 16MHz 68020 processor and 20 Mbytes of RAM yet could still handle large images. The Unix mmap system call is used to give the image processing functions a virtual-memory mapped image, leaving Unix to handle the paging-in of data from the file. This means the VIPS image file format was directly accessed from C in an efficient way with RAM being used by Unix to cache used memory pages automatically.

VIPS (VASARI Image Processing System) [16,17] has been used in all subsequent projects. It has functions to handle colour spaces as well as the usual image algorithms, with automatic parallel processing on SMP machines. The applications described below were implemented using ip, the VIPS GUI developed at the National Gallery. VIPS is now an open source project available at www.vips.ecs.soton.ac.uk.

# Applications of VASARI and MARC

We have split our imaging work into two parts. The VASARI scanner is used for technical studies of paintings, and the MARC camera is used by the photographic department at the National Gallery as a replacement for film photography.

The VASARI scanner has now imaged around 100 paintings. We are just finishing work on an improved version of the MARC camera: the new camera has a larger CCD array, peltier cooling, piezo micropositioning, and improved mechanical positioning. The MARC II can scan, assemble and calibrate a 10k x 10k image about 1 minute. By the end of 2001, the National Gallery will have imaged the 1500 most important paintings in the collection with the MARC II camera.

## Detecting colour change in paintings

We plan to use the collection of VASARI images as a foundation for long-term studies of colour change in paintings. We compared colour data from the VASARI scanner in the 1990s with spectrophotometric measurements made in the 1980s. We concluded that no colour changes occurred during 5-6 years on display [18].

## Detecting damage to paintings during transportation

This was another of the core aims of the VASARI project. Our colleagues at The Doerner Institute in Munich have conducted the research in this area. They have developed crack detection programs to highlight where changes may have occurred [19]. In a number of studies it has been shown that small changes can be detected after paintings have travelled to loan exhibitions [20]. Recently, improved techniques for registering and comparing images have been applied to a number of paintings loaned by the

Bayerische Staatsgemäldesammlungen, Munich. They found that most physical changes occurred at the edges of the paintings, but that one rather brittle painting showed more widespread changes [21].

## Conservation documentation

Colorimetric images of paintings at each stage of a conservation treatment provide an accurate, permanent record of the change in the appearance of a painting. Combined with resampling and some visualisation tools, they can also be used to allow comparisons to be made between colour before and after cleaning [22]. In a recent study, we made images of The Dead Christ supported by Two Angels by Carlo Crivelli (National Gallery, London No. 602) at seven stages during its cleaning and restoration.

As well as documenting the progress of cleaning and restoration, the images can be combined with spectrophotometric or colorimetric data relating to the properties of dirty or darkened varnishes to give an impression of how paintings might look once they have been cleaned.

5.4 Superposition of images

Many museums routinely use infrared reflectography to examine the preparatory drawings beneath the surface of a painting, and X-radiography to investigate the physical structure of a painting and changes made during its execution.

We have applied software developed in the VASARI project to the computer assembly of infrared reflectograms. These reflectograms are easier to make and are of a higher quality than was possible using photographic techniques [11]. Another useful application has involved using a visible-region image to tint an infrared reflectogram. This provides a clearer picture of the relationship between the underdrawing and the final painting [23]. X-radiographs have also been mosaiced using the VIPS software.

Resampling has also been used to compare different versions of the same painting, or to look for a common source, often a drawing, for two or more paintings. For example, a painting of Salome by Giampietrino (National Gallery No.3930) shows Salome holding the head of John the Baptist on a platter. Superpositition of this figure onto that of Cleopatra in another painting by Giampietrino, now in the Louvre, shows that the same drawing must have been used for both paintings [24].

5.5 Visualisation of colour change

Many paintings have changed in colour since they were produced. We have combined colorimetric images with spectrophotometric measurements from aged pigment samples to show how paintings might have appeared before they underwent colour changes.

One example of this application was the reconstruction of colours in The Annunciation by Zanobi Strozzi (National Gallery No.1406). The garments of two principal figures, the Virgin Mary and the Angel Gabriel, were painted using fugitive red lake pigments. We modeled the original colour in these pink robes using data obtained from the deterioration of red lake mixtures with white pigments [25]. Although these methods rely on objective criteria, the accurate measurement of colour and quantitative studies of change, such reconstructions are subjective representations of one of a range of possible appearances of a painting before deterioration.

## Pigment identification

We have investigated using VASARI multispectral images to identify pigments in paintings [26]. Although we were able to successfully identify some pigments, the spectral resolution and range of VASARI at the time we did the study was not sufficient for practical conservation use.

The seven-band images give enough information for a good CIE Lab measurement, but there is not enough detail to allow spectra to be identified accurately. Pigment spectra are usually rather similar, often very small intermediate maxima or “shoulders” are the only features distinguishing two materials with the same colour but different chemistry. Identification is also hampered by the frequent use of complicated pigment mixtures.

## Printing

We have used calibrated, large-format inkjet printers donated by Hewlett Packard (eg CFP2500) to produce colour-accurate life-size prints of paintings to act as reference images during conservation treatment. These accept CIE XYZ images and carry out calibration internally. They are commercially available and have been used in exhibitions elsewhere instead of moving a delicate painting. Their calibrated colour and 1:1 scale mean they can be placed next to contemporary works to provide a more faithful representation.

# VISEUM: putting the images on the Web

In 1996 the Viseum project worked on a client-server system [27] to make the large images produced in previous work accessible over the internet. Our solution used the Internet Imaging Protocol (IIP) with extensions to allow a Java client in a normal Web browser to fetch sRGB image tiles (64x64 pels) on demand in JPEG format for display. IIP standardised the way that programs request images from a server so that an IIP-aware browser can look at servers from different vendors. Thus it was possible to browse any size image in around 10 seconds over the Web.

A multiresolution TIFF file was used with full, half, quarter etc. resolutions stored as tiled JPEG images. By fetching only the tiles necessary for the specific view required at any one time the system became usable over the Internet at low bandwidths. An optional display colour profile (ICC) server maintains profiles on an ip address basis so that images can be transformed specifically for the user’s monitor rather than to sRGB. Figure 6 shows the IIP-viewer showing the low resolution view of Renoir’s The Umbrellas (National Gallery No.3268) with figure 7 showing the full resolution detail of this 7275x9982 pel image. Uncompressed it occupies 290 Mbytes and the JPEG-TIFF is 50 Mbytes.

# ACOHIR

The European project ACOHIR in 1996 applied the colour calibration from MARC with the Viseum image viewer to produce higher quality object views of objects [28]. These were captured with a high resolution Kodak digital camera and a motorised turntable. Objects could be seen from a wide range of angles at higher resolutions than available previously using Apple’s QuickTime-VR for example. The systems were used in archaeological and commercial applications and a scanner was made for the Louvre using a firewire-linked DCS560 camera capturing 3 x 36 views of 3k x 2k pels each.

## Related projects

The Artiste European project started in 2000 and will use colorimetric images as the basis for content-based retrieval of images, typically for picture library queries. It will also combine colour and shape queries for example, which are useful in conservation applications.

A digital version of the Alan Turing archive has been produced in 2000 which uses the multiresolution TIFF image format and server/viewer designed in Viseum to serve documents on the Web at www.turingarchive.org. The documents were captured using an EPSON GT10000 flatbed in the sRGB colourspace.

# Conclusions

In ten years we have implemented and continued to develop different imaging systems linked by a common image file format and image processing library. Digital imaging has become an established part of the National Gallery’s activities and is beginning to replace conventional photography. The VASARI system’s main use continues to be long-term monitoring of the condition of paintings and the technical analysis/documentation of the National Gallery’s collection. We are still actively developing the system, looking for improvements in image quality, spectral range and spectral reconstruction techniques.

Although the origins of these projects were in the scientific analysis of paintings, increased awareness of the usefulness of electronic images has led to a range of applications in addition to those we originally envisaged. Advances in CCD resolution have still not outdated the mosaicing techniques we developed. Colour calibration is still an active area of research as it is almost impossible to achieve an exact solution. We expect to increase precision further in the future using the latest advances in colour science.

# Acknowledgements

The MARC and VASARI projects were funded by the European Commission’s ESPRIT programme. VASARI involved: The Doerner Institute, Munich; Brameur Ltd. (UK); Birkbeck College London, Telecom Paris/ENST; Thomson-CSF LER, Rennes (F); TÜV-Bayern, Munich (D). The ESPRIT III project MARC involved: Thomson Broadband Systems, The National Gallery, Birkbeck College, The Doerner Institute Munich, Crosfield Ltd (UK), Hirmer Verlag (D) and Schwitter (Switzerland).

The new VASARI scanner GUI was written by Ruven Pillay while at the National Gallery funded by HP-Labs.

Thanks to Barco for advice and monitor models for colour display as well as sponsorship for their Calibrator.

9. References

- L. Bullock,  “Reflectance Spectrophotometry for Measurement of Colour Change”, National Gallery Technical Bulletin, Vol. 2, 1978, pp. 49–55.

- D. Saunders,  “Colour Change Measurement by Digital Image Processing”, National Gallery Technical Bulletin, Vol. 12, 1988, pp. 66–77

- Commission Internationale de l’Eclairage, “Recommendations on uniform color spaces, color difference equations, psychometric color terms”, Supplement No.2 to CIE Publication No. 15 (E-2.3.1), 1971 (TC-1.3) 1978.

- K. Martinez, J. Cupitt, and D. Saunders, “High resolution colorimetric imaging of paintings”, Proceedings of the Society of Photo-Optical Instrumentation Engineers, Vol. 1901, 1993, pp. 25 - 36.

- D. Saunders and J. Cupitt, “Image processing at the National Gallery: The VASARI project, National Gallery Technical Bulletin Vol. 14, 1993, pp. 72 - 85.

- D. Saunders, and A. Hamber, “From pigments to pixels: Measurement and Display of the Colour Gamut of Paintings”, Proceedings of the Society of Photo-Optical Instrumentation Engineers, Vol.1250, 1990, pp. 90 - 102.

- A. Burmester, J. Cupitt, H. Derrien, N. Dessipris, A. Hamber, K. Martinez, M. Müller, and D. Saunders, “The examination of paintings by digital image analysis”, Proceedings of the 3rd International Conference on non-destructive testing, microanalytical methods and environmental evaluation for study and conservation of works of art, Viterbo, Italy, 1992, pp. 201 - 214.

- A.R. Calmes, and E.A. Miller, “Registration and Comparison of Images Obtained at Different Times for Ageing Studies of the U.S. Constitution”, Proceedings of the Society of Photo-Optical Instrumentation Engineers, Vol. 901, 1988, pp.61.

- R. Lenz, “Calibration of a color CCD camera with 3000 x 2300 picture elements”, Proceedings of the Society of Photo-Optical Instrumentation Engineers. Vol.1393, 1990, pp. 104 - 111.

- C. S. McCamy, H. Marcus and J. G. Davidson, “A Color-Rendition Chart”, Journal of Applied Photographic Engineering, Vol. 2, No. 3, 1976, pp. 95 -99.

- R. Billinge, J. Cupitt, N. Dessipris, and D. Saunders, “A Note on an Improved Procedure for the Rapid Assembly of Infrared Reflectogram Mosaics”, Studies in Conservation, Vol. 38, 1993, pp. 92 - 98.

- R.P. Brent, “Algorithms for Minimization without Derivatives”, Prentice-Hall, 1973.

- R. Lenz, R. Beutelhauser and U. Lenz, “A microscan/macroscan 3 x 12 bit digital color CCD camera with programmable resolution up to 20,992 x 20,480 picture elements”, in Proceedings of the Commission V Symposium: Close range techniques and machine vision, Melbourne, Australia, International Archives of Photogrammetry and Remote Sensing, Vol. 30, No. 5, 1994.

- A. Burmester, L. Raffelt, K. Renger, G. Robinson and S. Wagini, Flämische Barockmalerei: Meisterwerke der Alten Pinakothek München; Flemish Baroque Painting: Masterpieces of the Alte Pinakothek München, Hirmer Verlag,  München, 1996.

- H. Derrien, “MARC, a new methodology for art reproduction in colour”, Information Services & Use. Vol. 13, No. 4, 1993, pp. 357-369.

- J. Cupitt and K. Martinez, “VIPS: An Image Processing System for Large Images”, Proceedings of the IS&T/SPIE Symposium on Electronic Imaging: Science and Technology, Very High Resolution and Quality Imaging, Vol. 2663, 1996, pp. 19 - 28.

- J. Cupitt, K. Martinez, “Image processing for Museums”, in Interacting with images, eds L. MacDonald and J. Vince, John Wiley, 1994, pp 133-147.

- D. Saunders, H. Chahine,  and J. Cupitt, “Long-term Colour Change Measurement: Some Results After Twenty Years”, National Gallery Technical Bulletin , Vol. 17, 1996, pp. 81–90.

- D. Saunders, L. Raffelt, J. Cupitt, and A. Burmester, “Recent applications of digital imaging in painting conservation: transportation, colour change and infrared reflectographic studies”, Tradition and Innovation: Advances in Conservation, ed. A. Roy, and P. Smith, IIC, London, 2000.

- A. Burmester, and M. Müller, “The Registration of Transportation Damages using Digital Image Processing”, Zeitschrift für Kunsttechnologie und Konservierung, Vol. 6, 1992, pp. 335–345.

- A. Burmester, and W. Wei, “All Good Paintings Crack: Nondestructive Analysis of Transport Damage of Paintings Using Digital Image Processing”, Proceedings of the 4th International Congress on Non-Destructive Testing of Works of Art, Berlin, 1994, pp. 114–126.

- H. Chahine, J. Cupitt, D. Saunders, and K. Martinez, “Investigation and Modelling of Colour Change in Paintings During Conservation Treatment”, Imaging the Past; British Museum Occasional Paper No 114, London, 1996, pp. 23–34.

- D. Saunders and J, Cupitt, “Elucidating Reflectograms by superimposing Infra-red and Colour images”, National Gallery Technical Bulletin, Vol. 16 1995, pp. 61 - 65.

- L. Keith, and A. Roy, “Giampietrino, Boltraffio and the Influence of Leonardo”, National Gallery Technical Bulletin, Vol.17, 1996, pp. 4-19.

- J. Kirby, D. Saunders, and J. Cupitt, “Colorants and Colour Change”, Early Italian Painting Techniques and Analysis, Maastricht, 1996, pp. 60-66.

- J. Thoma, J. Cupitt, and D. Saunders, “An investigation of the potential use of visible-region multispectral imaging for pigment identification in paintings”, Colour Imaging Science 2000, University of Derby, 2000, pp. 95-106.

- K. Martinez, J. Cupitt, and S. Perry. “High resolution Colorimetric Image Browsing on the Web”, Computer Networks and ISDN Systems. Vol. 30, 1998, pp. 399-405.

- K. Martinez and S. Perry and J. Cupitt, “Object browsing using the Internet Imaging Protocol”. Computer Networks, Vol. 33, 2000, p.803-810.

UNUSED REFS!!!

N. Ohta, “Colorimetric Analysis in the Design of Color Films: A Perspective”, Journal of Imaging Science and Technology, Vol. 36, No. 1, 1992, pp. 63-72.

- Farrell, J.E., Cupitt, J., Saunders, D., and Wandell, B.A., “Estimating Spectral Reflectances of Digital Images of Art”, Proceedings of the International Symposium on Multispectral Imaging and Colour Reproduction for Digital Archives, Society of Multispectral Imaging of Japan, Chiba, 1999, pp. 58-64.